## Slide 1: Influence of geometrical defects in the elastic-plastic failure of lattice materials
B. Boonkongchuen1, C.K. Lim1, W. Ronan2, E. Bele1
1University College London, Mechanical Engineering, London, UK
2NUI Galway, Biomedical Engineering, Galway, Ireland

## Slide 2: Introduction: Foams and Lattice Materials
1. Hybrids: Materials to fill holes in material property map
2. Most attractive region: Low ρ – High E (High σ)
[1]
[2]
[3]
[4]
[4]
[1] M. F. Ashby, Philos Mag, 2008 [3] D. J. Sypeck, Adv Compos Mat, 2005
[2] T. Miyoshi et al., Adv Eng Mat, 2000 [4] H. N. G. Wadley, Philos Trans Royal Soc, 2006

## Slide 3: Introduction: Stretching vs Bending-Dominated Architectures
Stretching- dominated deformation: Dictated by tensile tension/compression of constituent members, e.g. in compression, σ and E vary with [2].
[1] M. F. Ashby, Philos Mag, 2005; [2] V. S. Deshpande et al., Acta Mater, 2001
[1]
[2]
[2]
[1]
Maxwell’s stability criterion in 3D:
c struts, j joints, s states of self-stress, m mechanisms
c - 3j +6 = s – m
Bending-dominated deformation: Dictated by rotational rigidity of joints, e.g. in compression σ varies with and E varies with [2].

## Slide 4
[1]
Introduction: Ductility of Foams and Lattices
Large-scale deformation in tension present in e.g. tensile fibres of sandwich panels Prediction of ductility becomes significant
Tensile ductility of many foams is lower than that of the parent material, perplexing for bending-dominated structures
[1] W. Ronan, V.S. Deshpande, N..A. Fleck, Int J Solids Struct, 2016

## Slide 5
In This Talk
Mechanisms of tensile failure in additively manufactured periodic honeycombs (bending-dominated geometries)
Effect of geometric imperfections on tensile properties
Deformation Mechanisms In Tension
Effect of Macroscopic (periodic, semi-confined) Boundary Conditions
Influence of Strut Aspect Ratio
Geometric Perturbations
Inclusions
Missing Cell Walls (cracks)

## Slide 6
Overview
Introduction to cellular materials
Tensile response of periodic honeycombs
  Effect of relative density: periodic boundary conditions
  Towards experimental tests: specimen size effects
Tensile response of semi-confined experimental honeycombs
Effect of geometrical perturbations on ductility and tensile strength
Effect of crack and inclusion size on tensile ductility

## Slide 7
FE Model: Honeycombs with Periodic BCs
Finite Element Model: ¼ of a 13x13 unit cell RVE modeled
Symmetry BCs on bottom/left boundaries. u22 prescribed on top boundary. Plane strain conditions.
Solver: ABAQUS Standard
Around 10 through-thickness elements

## Slide 8
FE Model: Honeycombs with Periodic BCs
Relative density:
Strut Aspect Ratio

## Slide 9
FE Model: Honeycombs with Periodic BCs
Material: fitted to SLS Nylon experimental tests (2-Direction)
with: , , , , .
Constituent Material: Nylon (SLS Manufacturing)

## Slide 10
Tensile Response of Honeycombs with Periodic BCs
Low Relative Density Model ( )
1) Elastic Bending
2) Plastic Bending
2) Lock-up

## Slide 11
Tensile Response of Honeycombs with Periodic BCs
1) Elastic Bending
2) Plastic Bending

## Slide 12
Tensile Response of Honeycombs with Periodic BCs
Macroscopic tensile failure strain defined at first occurrence of:
lock-up in low density honeycombs,
tensile necking in high density honeycombs
Replication of Boundary Conditions in Experimental Tests?
Initiation of Lock-Up
Tensile Necking
Material εf

## Slide 13
Additively Manufactured Honeycomb Geometries
Honeycomb specimens fabricated with selective laser sintering – base material Nylon powder. Resolution: 0.5 mm
Geometry design criteria:
a) Plane strain conditions:
b) Minimisation of lateral constraints in top nodes
c) Minimisation of specimen size effects
Free variables: and

## Slide 14
Effect of Lateral Constraints (Ligament Size d/H)
Rho = 0.2 chosen for illustration; similar parametric studies were done on other relative densities.

## Slide 15
Effect of RVE Size (R/l)
Rho = 0.2 chosen for illustration; similar parametric studies were done on other relative densities.

## Slide 16
Effect of Lateral Constraints and RVE Size
Mechanisms of failure: strut lock-up for low density honeycombs, tensile necking for high density ones
Introduction of ligaments preserves these mechanisms
Have not eliminated the effect of lateral constraints, but due consistent differences can predict ductility in periodic conditions

## Slide 17
Overview
Introduction to cellular materials
Tensile response of periodic honeycombs
  Effect of relative density: periodic boundary conditions
  Towards experimental tests: specimen size effects
Tensile response of semi-confined experimental honeycombs
Effect of geometrical perturbations on ductility and tensile strength
Effect of crack and inclusion size on tensile ductility

## Slide 18
Tensile Response of Additively Manufactured Periodic Honeycombs
Static tensile tests carried at a remote strain rate of 10-3 s-1
Tests recorded with a DSLR camera (frame acquisition rate 50 Hz)
Image analysis (Matlab) used to calculate macroscopic strains in the honeycomb assembly, and local strut strains

## Slide 19
Tensile Response of Additively Manufactured Periodic Honeycombs
Characteristic deformation mechanisms: similar to numerical calculations
Notes: add honeycomb struts with labels
add tensile limit line
make this two slides – add conclusions

## Slide 20
Tensile Response of Additively Manufactured Periodic Honeycombs
Low-density honeycombs: Plastic bending failure precedes local tensile strain
High-density honeycombs: Macrosopic failure due to achievement of local tensile strain
Strut B
Strut B
Strut A
Strut A
Strut B
Notes: add honeycomb struts with labels
add tensile limit line
make this two slides – add conclusions

## Slide 21
Overview
Introduction to cellular materials
Tensile response of periodic honeycombs
  Effect of relative density: periodic boundary conditions
  Towards experimental tests: specimen size effects
Tensile response of semi-confined experimental honeycombs
Effect of geometrical perturbations on ductility and tensile strength
Effect of crack and inclusion size on tensile ductility

## Slide 22
Effect of Geometrical Perturbations on Ductility and Tensile Strength
Geometrical perturbations generated by displacement of nodal junctions on an arbitrary position in a circle of radius
Nodal perturbation magnitude characterized by
Honeycomb with rel. density = 0.2 chosen as baseline
Notes: add arrows
add ref

## Slide 23
Effect of Geometrical Perturbations on Ductility and Tensile Strength
Both tensile ductility and strength shortcut by nodal perturbations
Moderate reductions: ≈ 0.7 for δ/l = 0.4
Notes: Arrows to show trends
Video

## Slide 24
Overview
Introduction to cellular materials
Tensile response of periodic honeycombs
  Effect of relative density: periodic boundary conditions
  Towards experimental tests: specimen size effects
Tensile response of semi-confined experimental honeycombs
Effect of geometrical perturbations on ductility and tensile strength
Effect of crack and inclusion size on ductility and tensile strength

## Slide 25
5. Effect of Crack and Inclusion Size on Ductility and Tensile Strength
Missing cells (cracks) or inclusions, of size 2a, spaced a distance 2H apart are explored
Cracks created by nb broken walls:
Inclusions created by nf filled cells:
All tests carried on RVE with and (13x13 unit cells)

## Slide 26
5. Effect of Crack Size on Ductility and Tensile Strength
Macroscopic tensile strength and ductility controlled by tensile fracture of crack tip ligament
Ductility reduced by less than crack/specimen size ratio
Notes: Trends, Location of failure

## Slide 27
5. Effect of Inclusion Size on Ductility and Tensile Strength
Macroscopic tensile strength and ductility controlled by tensile fracture of confined ligaments
Ductility reduced by more than crack/specimen size ratio
Notes: Trends, Location of failure

## Slide 28
6. Summary of Influence of Imperfections
Presence of all 3 types of imperfections shortcuts ductility and tensile strength
In bending-dominated geometries: largest effects on tensile strength strength reduction is caused by presence of cracks
Tensile ductility shortcut is most sensitive to hard inclusions
Cooperative influence of multiple imperfection types is very possible
Notes: Trends, Location of failure

## Slide 29
Acknowledgements
Notes: Trends, Location of failure